## Slide 1
EG7030 — MSc Electric Vehicle Engineering | UEL
Duty Cycle-Aware Battery Degradation
Analytics for EV Fleet Applications
Supervisor Meeting — Progress Update
Student:
Usha Rani V. | u2965962
Supervisor:
Dr. Abdulrahman Albar
Date:
14 July 2026
COMPLETED STAGES
S1
Data
Preprocessing
S2
Duty Cycle
Features
S3
EDA &
FSI Analysis
Notes: Good [morning/afternoon] Dr. Albar. Thank you for your time today. My dissertation investigates how different EV fleet duty cycles degrade NMC batteries differently, and proposes a Fleet Severity Index (FSI) as a novel contribution to quantify real-world battery stress. Today I want to share what I have completed over the last few weeks — Stages 1 through 3 are complete — and get your guidance on a few key decisions before I move into the ML modelling phase.

## Slide 2
What Has Been Completed
01
Data Collection & Preprocessing
• 4 lab datasets: NASA, Oxford, CALCE CS2, SP20
• 9,031 cycles extracted — SoH, DoD, C-rate, FSI per cycle
• CALCE Arbin cumulative counter decoded correctly via delta-extraction
9,031
Lab Cycles
02
Duty Cycle Feature Extraction
• 553 Fleet DNA trips: KI, RPA, CVI, RBF, DCSS, FSI computed
• CALCE dynamic profiles: DST / FUDS / US06 / BJDST at 3 temperatures
• Master ML dataset: 9,031 rows x 24 features + health labels
553
Fleet Trips
03
EDA + Novel FSI Validation
• 3-fleet comparison: Delivery vs Transit Bus vs Refuse Truck
• Transit buses: KI = 1.86 (2.8x higher than delivery trucks)
• FSI correctly ranks fleet severity — validated across all vocations
3
Fleet Types
FSI Formula
KI
0.30
Kinetic
Intensity
DoD
0.25
Depth of
Discharge
T
0.25
Temperature
Stress
Cpk
0.20
Peak
C-rate
Notes: STAGE 1 — Data Preprocessing: I collected four lab battery datasets and extracted per-cycle capacity measurements. The trickiest part was the CALCE Arbin cycler which stores cumulative capacity — I had to implement a delta-extraction approach to get the correct per-cycle values. Total: 9,031 validated lab cycles. STAGE 2 — Duty Cycle Feature Extraction: I processed 553 real-world delivery truck trips from NREL Fleet DNA, computing Kinetic Intensity, RPA, CVI, RBF, DCSS, and FSI for each trip. I also processed the CALCE dynamic current profiles (DST, FUDS, US06, BJDST) at 0, 25, and 45 degrees C. The master ML dataset has 9,031 rows and 24 features. STAGE 3 — EDA + FSI Validation: The novel contribution is the Fleet Severity Index shown on the right. I extended the analysis to three fleet types — delivery trucks, transit buses, and refuse trucks — all from Fleet DNA. Transit buses have the highest Kinetic Intensity (mean 1.86 vs 0.66 for delivery), and their FSI is 70% above the lab test baseline. This validates that lab constant-current tests under-represent real fleet degradation.

## Slide 3
Key Findings — FSI Validation across 3 Fleet Types
9,031
Lab cycles
processed
3
Fleet types
compared
+70%
Transit FSI above
lab baseline
KI=0
Lab tests miss
all kinetic stress
Fleet Type
Trips / Vehicles
KI Mean
FSI Mean
vs Lab
Proj. SoH
Lab (CC baseline)
9,031 cycles
0.000
0.305
—
Measured
Delivery Trucks
553 / 36 veh
0.661
0.450
+47.6%
~77% (EOL)
Transit Buses
472 / 19 veh
1.862
0.518
+70.1%
~86% (Degraded)
Refuse Trucks
387 / 39 veh
1.077
0.456
+49.8%
~79% (EOL)
KI is the key gap
Lab CC tests have KI=0. Real fleets range 0.66-1.86. Lab underestimates degradation by 47-70%.
FSI multi-component
Refuse trucks have higher KI than delivery but same FSI — IRMS lower. FSI correctly weights all stress factors.
Counter-intuitive result
Transit buses project best SoH (86%) despite highest KI — because FSI, not KI alone, drives degradation.
Notes: HEADLINE STAT — +70% FSI above lab: Every real-world fleet operates at significantly higher Fleet Severity Index than any lab test. The biggest driver is Kinetic Intensity — KI is zero in all constant-current lab tests, but ranges from 0.66 to 1.86 across the three fleet types. THREE-FLEET COMPARISON: - Delivery trucks: 553 trips, 36 vehicles, KI mean 0.66, FSI mean 0.450, projected SoH ~77% - Transit buses: 472 trips, 19 vehicles, KI mean 1.86, FSI mean 0.518, projected SoH ~86% - Refuse trucks: 387 trips, 39 vehicles, KI mean 1.08, FSI mean 0.456, projected SoH ~79% COUNTER-INTUITIVE FINDING: Transit buses have the highest KI but project the healthiest batteries. Their IRMS (root-mean-square current) is lower than delivery trucks because transit buses run at consistent low speeds between stops. This shows FSI correctly integrates multiple stress factors, which KI alone cannot do. NOVEL CONTRIBUTION: The FSI framework bridges lab and fleet by treating KI as a measured duty-cycle input. Stage 5 SHAP analysis will quantify exactly how much each component contributes to SoH prediction — validating the 30/25/25/20 weighting scheme.

## Slide 4
Next Steps & Questions for Discussion
UPCOMING STAGES
4
Stage 4
ML Models
This week
RF, XGBoost, LSTM on master dataset — 9,031 rows x 24 features
Health classification + SoH regression, replace placeholder results
5
Stage 5
SHAP Explainability
Next week
TreeExplainer on XGBoost — quantify KI vs DoD vs T importance
Validates FSI weighting (30/25/25/20) as novel contribution
6
Stage 6
PyBaMM Simulation
Late July
SPMe physics model, NMC-811 Chen2020 parameters
Validates lab degradation trends with electrochemical physics
7
Stage 7
FSI Finalisation + Writing
August
Replace placeholder ML numbers with real computed values
FSI formula alignment + fleet severity ranking
QUESTIONS FOR DISCUSSION
Q1
FSI Formula Alignment
Dissertation draft uses a different FSI formula based on SoH prediction. Should I align with the KI-based formula computed here, or keep both versions?
Q2
Class Imbalance in ML
Master dataset is highly imbalanced:
End-of-Life: 7,100 | Degraded: 1,099 | Healthy: 832
Should I use SMOTE oversampling or class weights?
Q3
4th Real-World Dataset
Considering Mendeley real EV driving dataset (1-year BEV data with measurable SoH). Worth adding to validate FSI projections with actual capacity results?
Notes: STAGE 4 — ML Models (This week): I will train Random Forest, XGBoost, Gradient Boosting, SVM for classification (Healthy / Degraded / End-of-Life) and LSTM for SoH regression prediction. The dissertation currently has placeholder accuracy numbers (XGBoost 93.7%, LSTM R2=0.981) which I need to replace with real computed values. STAGE 5 — SHAP (Next week): SHAP TreeExplainer on the trained XGBoost model will quantify whether KI has the highest feature importance for SoH prediction — which would validate the 30% weight I gave it in the FSI formula. QUESTION 1 — FSI Formula: The dissertation draft uses: FSI = 0.25*DCSS + 0.35*(1-SoH_pred) + 0.25*dSoH_rate + 0.15*EFC/EFC_max. My computed FSI uses KI, DoD, T, and C-peak. I need your guidance on which to use as the primary FSI definition going forward. QUESTION 2 — Class Imbalance: The ML dataset has 7,100 End-of-Life rows vs only 832 Healthy rows. This will bias the classifier. I am planning to use SMOTE to oversample the minority classes, but wanted to confirm this is the right approach for time-series battery data. QUESTION 3 — Mendeley Dataset: Currently all fleet SoH estimates are projected from the lab regression — not directly measured. Adding a real-world EV dataset with measurable SoH would strengthen the validation chapter. Is this worth the extra preprocessing time, or should I focus on completing Stages 4-7 first?